TANK PAINT LINE WASH

PRETREATMENT PARAMETERS

|  | STAGE 1 | STAGE 2 |
| --- | --- | --- |
| PRODUCTS - OAKITE | CRYSCOAT 347C | 200-303-001 |
| pH ADDITIVE | ADJUST M: AUTO. | N/A |
|  | EXPROX 714: MAN. |  |
| SPRAY ZONE | CABINET WASH | CABINET WASH |
| CONCENTRATION - TARGET | 4.2% | 2.5% |
| CONCENTRATION - RANGE | 4.0 - 4.4% | 2.0 - 2.75% |
| pH - TARGET/RANGE | 4.75 pH/ 4.5 - 5 pH | 8 - 10 pH |
| TEMPERATURE | 49 - 55 C/120 - 130 F | 21 - 60C/70 - 140 F |
| NOZZLE PRESSURE * | East/West 20 - 25 PSI\North/South Clusters 45 - 50 PSI | East/West 20 - 25\North/South Clusters 45 - 50 |
| TANK CAPACITY | 3591 LITRES | 3591 LITRES |
| LITRES TO CHARGE | 150 LITRES | 90 LITRES |
| MAXIMUM LINE SPEED | N/A | N/A |
| DUMP SCHEDULE (TDS-PPM) | 4 - 6 MONTHS | (MAX 530 PPM |

ALL PARAMETERS ARE TO BE KEPT AS CLOSE AS POSSIBLE TO THE TARGETS FOR OPTIMUM PERFORMANCE.

IMMEDIATE CORRECTIVE ACTION MUST BE TAKEN IF A BATH IS OUT OF RANGE.

* Note:  All rinse pressure parameters are:  East/West 30 - 35 PSI/North/South Clusters 50 - 60 PSI.