5 STAGE WASH PRETREATMENT PARAMETERS.

|  | Stage 1 | Stage 2 | Stage 3 | Stage 4 | Stage 5 |
| --- | --- | --- | --- | --- | --- |
| Products - Oakite | Inpro-Clean 1300 | Rinse | Cryscoat 347C | Rinse | 200 – 303 - 001 |
| pH Additive | N/A | Fresh water - Stage 4 overflow | Adjust OX -automatic Enprox 714 - manual | Fresh Water | N/A |
| Spray Zone | 13’ | 10’ | 20’ | 7’ | 7’ |
| Conc. - Target | 3.5% | N/A | 4% | N/A | 1.25 |
| Conc. - Parameters | 3 - 4% | Max. 0.6 Target 0.1 | 3.8 – 4.2% | Max. 0.6 | .75 – 1.5% |
| pH - Target/Range | 8 - 10 pH Target 9 | Monitor | 4.35 - 4.7 pH | Monitor | N/A |
| Temperature | 60 - 66°C/140 - 150°F | Ambient | 49 - 55°C/120 - 130°F | Ambient | 43 – 52°C |
| Nozzle Pressure (PSI) | 25/25 | 15 | 17 | 15 | 10 |
| Tank Capacity (Litres) | 23,300 litres | 13,800 litres | 13,800 litres | 9600 liters | 9600 liters |
| Litres to Charge | 815 litres | N/A | 552 liters | N/A | 120 liters |
| Maximum Line Speed | 6’/min. | 6’/Min. | 6’/min. | 6’/min. | 6’/min |
| Dump Schedule (TDS) | 4 - 6 months | Max. 530 TDS or every month | 4 - 6 months | Max. 530 TDS or Every Month | Max. 530TDS |

*	“Target” is the optimum desired concentration.

**	“Parameter” is the maximum allowable variance of concentration.  Corrective action must be taken immediately when the concentration nears (depends on the stability of the solution) the parameter.  If the wash solution goes out of any of the above parameters contact the Front Line Supervisor immediately and take the appropriate corrective action.