## 5500 CADDY CART & HITCH

## QUALITY ASSURANCE PROCEDURE

# Attachments:	5500 Caddy Cart/Hitch Q.A. Checklist

Pretreatment/Cure Testing Diagrams

Mil Testing Diagram

### Hatch & MEK Testing Diagrams

References:	PLS 802 Pretreatment Quality Assurance Procedure

PLS 205 Powder Paint Cure Quality Assurance Procedure

This procedure explains and outlines the quality assurance checks for the 5500 Caddy Cart & Hitch.

RESPONSIBILITIES ARE AS FOLLOWS:

- The Pretreatment Operator is responsible to:

- Record on the 5500 Caddy Cart & Hitch Q.A. checklist

- Name, Date and Time

- Pretreatment conditions (within 1.5 hours of the cart & hitch being pretreated in the wash)

- Water Break Test result

- Take the checklist to the painters as soon as possible

- The Painters are responsible to:

- Receive the Caddy Cart & Hitch Q.A. checklist from the pretreatment operator

- Perform and document the following testing (all locations of testing must be documented on attached diagram)

- White Rag Test

- Phosphate Test using Test Solution #47

- Flash Rust N/C

- Chemical Run N/C

Note:  a) and b) are to be done on the first cart & hitch of each shift while c) and d) are to be checked on all parts on the line randomly throughout the day.

- Document the following:

- Painted by (indicate both north and south side painter employee numbers)

- Cure conditions (oven temp., track speed and any non-conformances)

- Initiate and document the cart & hitch ID #s

- Place the magnetic temperature gauge on the hottest part of the caddy.  When the temp. on the gauge reads 100ºF or less, then you may start to take mil readings.  Any mil readings taken above this temp. may result in damage to the probe.

- Perform and document the following inspections/testing:

- Pinhole Classification (visual inspection based on Powder Paint Cure Quality Assurance Specification)

- Gloss Rating (visual inspection based on Powder Paint Cure Quality Assurance Specification)

- Mil Thickness (document mils on appropriate diagram with min. 24 readings on hitch & min. 40 readings on cart / circle mil readings that are showing opposite side of beam)

Note:	Ensure gauge is calibrated properly using an 11 gauge panel that has been blasted and washed within 5 days.

- Hatch Test Results (locations as per diagram and performed as per Powder Paint Cure Quality Assurance Specification)

- MEK Test Results (locations as per diagram and performed as per Powder Paint Cure Quality Assurance Specification)

- Paint Non Conformance (note any contamination, etc.)

- Document for repaint:

- Circle ‘yes’ or ‘no’

- If ‘yes’, document reason for repaint, complete appropriate repairs as per repaint standards and document in Repaint Record section on checklist

- Inspected by . . . sign it (painter/inspector).

- Touch up Hatch & MEK test marks with 5:1 urethane paint that has been catalyzed.

- The caddy cart & hitch must be signed off as good and passing all inspections/testing by the (Company).

- Sticker the cart & hitch with ID #s and put checklist with caddy & hitch for release to assembly.

5500 Caddy Cart & Hitch Quality Assurance Checklist

Date:  __________________________			Time: _______________am / pm

Sequence Number: _______________ 			Cart / Hitch

PRETREATMENT

Wash Operator: __________________			Employee ID#: ______________

PREATREATMENT CONDITIONS

Inproclean 1300        H2O Rinse               Cryscoat 347C           H2O Rinse               H2O Rinse

%: ______             %: ______               %: ______                %: _______      %: _______ pH: ______            pH: ______             pH: ______               pH: _______   pH: _______        temp: ______ C     temp: ______C   temp: ______C  temp: _______C  temp: _______C

psi: ______   psi:  ______   psi: ______  psi: _______   psi: _______

tds: _______    tds: _______            tds: _______

PRETREATMENT TESTING

Water break (visual):  _________

Comments:  ________________________________________

Phosphate (T.S. #47): _________

Comments:  ________________________________________

White rag test:  _________

Comments:  ________________________________________

Flash rust N/C:          ____________________________________________________________

Chemical run N/C:     ____________________________________________________________

(All testing locations to be documented on appropriate diagram.)

PAINT

Painted by: (north) _____________________   Employee ID#: ________________

Painted by: (south) _____________________   Employee ID#: ________________

CURE CONDITIONS

Oven Temp: ______________                         Track Speed: ____________ft/min.

Comments:  ____________________________________________________________________

CURE TESTING

Pinholes Classification:  ___________                    Paint Mils:

Hatch Test Result:          ___________                    Minimum:  ______________

MEK Test Result:           ___________                    Maximum:  ______________

Gloss Rating:                   ___________                   Average:     ______________

Paint non-conformance: __________________________________________________________

______________________________________________________________________

Repaint:    NO

YES

Reason:  _____________________________________________________

Inspection by: ___________________________

Employee ID#:  _____________________

Signed off by: ___________________________

REPAINT RECORD

Area(s) repainted:  _______________________________________________________________

Reason:  ______________________________________________________________________

Description of work:  ____________________________________________________________

Rechecked/ signed off by:  ________________________

Employee ID#:  __________________

Time/Date Started:    ________________________

Time/Date Finished:  ________________________

Total Time to Fix:      ________________________

## 5500 CADDY CART/HITCH HATCH & MEK LOCATIONS

## 5500 CADDY CART/HITCH MIL TESTING LOCATIONS

## 5500 CADDY CART/HITCH PRETREATMENT TEST LOCATIONS

W - White Rag Test

F   - Flash Rust

C   - Chemical Run

P   - Phosphate Test

## 5500 CADDY CART/HITCH MIL TESTS

Cart:

Low: _____

High: _____

Avg.: _____

Hitch:

Low: _____

High: _____

Avg.: _____

# Text boxes

2

1

4

3

5

6

7

8

2

3

4

5

6

7

1

8

9

11

12

13

14

10

Hatch

MEK

Hatch & MEK