DRY OFF AND CURE OVEN

START UP AND SHUTDOWN

PROCEDURE

A.	SYSTEM START UP

Note:  Ovens should be started at 6:45 a.m. at the latest or at least 1 hour before the beginning of the shift.

- Remove dock lights and close access doors (cure oven).

- General

  - Turn the main disconnect on after weekends and lockouts.  This switch will wear out quickly if it is turned on and off numerous times.  It is not necessary to turn it on and off except for the two reasons listed above.

  - The white power on light will come on.

- Dry Off System Start Up

  - Start all 7 fans.

    - Push circulating fan start, green light will come on.

    - Push exhaust fan start, green light will come on.

    - Push entry air seal fan start, green light will come on.

    - Push exit air seal fan start, green light will come on.

    - Push cooling tunnel supply start, green light will come on.

    - Push cooling tunnel exhaust start, green light will come on.

    - Push dry off cool down supply start, green light will come on.

If all 7 lights are on fans are operating.

Note:  If any lights do not come on contact Supervisor or Electrical Maintenance.

  - Igniting the burner.

    - Push the burner start button.

    - Burner fan start light comes on.

    - Purging will automatically start.

    - When purge light comes on burner will purge for 12 minutes.

    - When purge is complete pilot light comes on.

    - Do not push main flame on bottom; this will be done by the Paint Crew Staff when they come in.

- Cure Oven System Start Up

  - Fans

    - Push zone 1 circulating fan start, green light comes on.

    - Push zone 2 circulating fan start, green light comes on.

    - Push exhaust fan 1 start, green light comes on.

    - Push exhaust fan 2 start, green light comes on.

    - Push zone 3 circulating fan start, green light comes on.

    - Push entry air seal fan start, green light comes on.

    - Push exit air seal fan start, green light comes on.

  - Igniting the Burners

    - Push burner start, green light comes on.

    - Yellow purge light comes on.  Burner will purge for 12 minutes.

    - “Pilot On” light comes on.

    - Do not push main flame on button; this will be done by Paint Crew staff when they come in.

B.	SYSTEM SHUTDOWN

- Access doors should be open on cure oven.

- Check temperatures of burner approximately one hour after end of evening shift (about 1:00 a.m.).

- Main flame and burner lights should already be off.

- If temperatures are below 80(C the entire fan can be turned off.

- Main disconnect should be left on unless you are locking out the panel.

Note:	Emergency stop buttons are for emergency only.