OILY MATERIAL PRE-LOADING

FOR ALL PAINT LINE

Warning:	Failure to understand and follow these procedures may result in:

a.	Safety Hazard

b.	Blast Machine dust collector fire

c.	Pre-treatment wash system contamination

d.	Coating Failure

1.	Before loading any items on the paint track they must be checked for an oil coating on the item.  Any item which has oil on it to the extent that the item appears “wet” must be pre-washed before loading on the paint track.  Items which have a “moist” but not a “wet” appearance are exempt from this prewash procedure and may be loaded “as is”.

2.	Items to especially watch out for are:

a.	Any items which have been wedged.

b.	Tubing etc. which comes in pre-coated in oil.

c.	Hardware items which need oil to be pretested, for example hydraulic valves etc...

3.	Reasons why oil needs to be washed off items prior to loading are:

a.	Oil drips on floor along track causing the floor to become slippery which is a safety hazard.

b.	Oil residue mixed with dust in the Blast Machines’ dust collector causes the filters to plug and will cause spontaneous combustion.

c.	Oil going through the pre-treatment wash system will contaminate the system.

4.	Items which need to be washed must be taken to the Air Seeder Tank Pressure Wash Area.  This procedure must follow all the following steps in this order:

Personal Protective Equipment (needed when handling and spraying fleet line).

-Chemical respirator Niosh approved organic vapour respirator with a dust and 			mist prefilter.

- chemical safety goggles.

- chemical resistance gloves and clothing to prevent skin contact.

b.	(Company) Supervisor from Paint Loading to contact (Company) Supervisor in tank wash and arrange for a time when the wash area will become available, and the quantity and description of items to be washed.

c.	(Company) employees to get the parts ready for washing, example: hang on racks etc.

d.	(Company) employee to transport items to wash area and contact wash employee on arrival and location of items.

e.	Check the level of fleet line and water mixture in the fleet line pump.  If empty, contact tank Wash (Company) Supervisor and he/she will look after getting the fleet line pump with fleet line and water...

f.	The fleet line and water mixture should be as close to 50% fleet line and 50% water as possible in order to get the items cleaned properly.

g.	(Company) employee is to wash each item carefully with fleet line and water mixture when finished turn the pump off.

h.	Pressure wash the items with water to rinse off the fleet line and water mixture.

i.	Once the items are completed the (Company) employee must remove the items from the manual wash area and clean the area up immediately before leaving the tank wash area.

5.    Parts that have been wedged or formed using oil or lubricants that are not    compatible with water must be washed with fleet line and water mixture prior to loading the parts on the paint line.  Parts that have been wedged or formed using aqueous solutions do not have to be washed prior to loading.